# CERTIFICATE  OF  ANALYSIS

Glass fabric 80 g/m2 - plain

| Product Name | EW80-12X12-1000 | Test By | Q/C |
| --- | --- | --- | --- |
| Manufacture Number | : NT3-416 | Sampling From | : Weaving cloth Dept. |
| Production Date | : APRIL12, 2008 | Product Grade | : “ A “ Grade |
| Lot Number | : JDM08045 | Purchase Order No. | JDTX8-328 |
| Lot Capacity | :5000m | Container No. | TOLU3401652/390942PART |

General Data:

| Glass Type | :EGLASS CLOTH | Filament Diameter | : 9μm |
| --- | --- | --- | --- |
| Density | : 12×12ends/cm | Sizing | Epoxy compatible |
| Yarns use | Warp | : EC9-33X1TEX | Color | White |
|  | Weft | EC9-33X1TEX |  |  |

Properties For Control Report:

|  | Accepted Standards | Test Results |
| --- | --- | --- |
|  | Standard No. | Standard Value | Average Value | Result |
| Sizing | GB/T 9914.2-2001 | 0.4%-0.8% | 0.6% | PASS |
| Moisture content (%) | GB/T9914.1-2001 | ≤0.20 | 0.06 | PASS |
| Density (ends/cm) | Warp | As per our contract | 12.0±1 | 12.2 | PASS |
|  | Weft | As per our contract | 12.0±1 | 12.2 | PASS |
| Tensile strength (N/25*100mm) | Warp | As per our contract | ≥300 | 396 | PASS |
|  | Weft | As per our contract | ≥300 | 458 | PASS |
| Mass(g/m2) | As per our contract | 80±8 | 80 | PASS |
| Width(cm) | GB/T7689.3-2001 | 100±1.0 | 100.1 | PASS |
| Length(m) | GB/T7689.3-2001 | 100±2.0 | 100.0 | PASS |

Test Conditions:

Room Temperature	: 25°C

Humidity	: 48 %

Test Conclusions:

- Passed

Havel Composites CZ , s.r.o.,Svésedlice 67,Přáslavice,783 54

Tel.: 585 129 010,Fax 585 129 040,

www.havel-composites.cz, info@havel-compositec.cz